## Slide 1: Shape Conformable Battery Pack (Team #15)
Sponsor: Dr.Zheng
Advisor: Dr.Shih
Team Members:
David Goss
Roberto moutran
Jenna Pine
Brian rainbeau
Niraj Thakker
Jianchen Yu
04/17/2014

## Slide 2
David Goss 1
Executive Summary
Brief Overview
Manufacture of Lithium Cobalt Cells
Prototypes
Testing
Prototype Demos
Hazards
Conclusion
Future Recommendations

## Slide 3
David Goss 2
Brief Overview
Design a shape conformable battery pack to fly a Remote-Controlled (RC) Plane

## Slide 4
David Goss 3
Objectives and Goals
Build proof-of-concept prototype to justify design.
Design should be modular.
Sustain flight for 5 minutes.
Design should be safe.

## Slide 5
Design Concept 1
David Goss 4
Large thin cells.
Bend around the wing.
Protective casing needed.

## Slide 6
Design Concept 2
David Goss 5
Multiple cells embedded in origami sheet.

## Slide 7
Roberto Moutran 6
Manufacture of Lithium Cobalt Cells (LiCo)
Single layer cell (1 cathode, 1 anode)
Raw Materials:
  Aluminum foil coated by LiCoO2 cathode sheet
  Double-sided copper foil coated by CMS graphite anode sheet
  Lithium Hexafluorophosphate (LiPF6) liquid electrolyte
  Celgard separator film

## Slide 8
Roberto Moutran 7
Manufacture of LiCo Cells
Electrode preparation:
Dimensions:
8.5cm x 5cm
Thickness: 0.2 mm Cathode
0.1 mm Anode

## Slide 9
Roberto Moutran 7
Manufacture of LiCo Cells
Electrode preparation:
Good Electrodes
Overcut
Undercut

## Slide 10
Roberto Moutran 8
Manufacture of LiCo Cells
Cell folding:

## Slide 11
Roberto Moutran 8
Manufacture of LiCo Cells
Cell folding:
Good Pouch
Bad Pouch
A good pouch keeps the electrodes close but fully isolated from each other
Contact between electrodes in bad pouch – short circuit

## Slide 12
Roberto Moutran 9
Manufacture of LiCo Cells
Aluminum casing:
Aluminum laminated film for pouch cell casing

## Slide 13
Roberto Moutran 9
Manufacture of LiCo Cells
Aluminum casing:
Additional space left for formation process

## Slide 14
Roberto Moutran 10
Manufacture of LiCo Cells
Glue strips lined up over sealing spot
First Sealing Pass:
Seals

## Slide 15
Roberto Moutran 12
Manufacture of LiCo Cells
Electrolyte and Rest Period:
3 pipettes of LiPF6 liquid electrolyte
Enough electrolyte to cover cell inside without leaking
Two hour rest period to allow cell to fully soak

## Slide 16
Roberto Moutran 13
Manufacture of LiCo Cells
Clamping, Top Seal and Formation:
Clamping:
Keeps electrodes in contact with electrolyte
Pushes out air and excess fluid
Formation: Charge/discharge cycling with battery analyzer.

## Slide 17
Roberto Moutran 14
Manufacture of LiCo Cells
Formation Process:
  Three cycles at slow discharge rate, ~24 hours
  Cycle time will depend on battery quality
  Charge/discharge cycle increases temperature in battery
  Extra gas and excess electrolyte is pushed away from the cell into the long end of the aluminum foil

## Slide 18
Roberto Moutran 15
Manufacture of LiCo Cells
Cut and Final Vacuum Seal
Final LiCo Battery

## Slide 19
Roberto Moutran 16
Manufacture of LiCo Cells
Additional Problems:
  Machinery issues
  Humidity
  Time
  Channel limitation on analyzer
  Variability

## Slide 20
Large Bent Batteries
  Connect two packs in series with bullet connectors to increase voltage.
  Put battery packs in nylon sheets in order to protect and reinforce the batteries.
  Wrap the battery packs around the airfoil and fix them with rubber bands.
Prototype
Jianchen Yu 17

## Slide 21
Origami Battery Pack
  Connect 7 single batteries in parallel to supply enough capacity and two packs in series to supply enough voltage.
  Insolate the terminals with electrical tape and mark anodes with red tape while cathodes with black tape.
Prototype
Jianchen Yu 18

## Slide 22
Origami Battery Pack
  Place batteries in set of 7 at a certain interval to a sheet of contact paper to guarantee the bendability.
  Solder connectors in an array to connect anode terminals and cathode terminals relatively and strengthening the master connectors with electrical tape.
Prototype
Jianchen Yu 19

## Slide 23
LiCo Battery Packs
  Connect 2 single batteries in parallel and two packs in series following the same process as origami design.
  Wrap them around both sides of the airfoil and clamp them with plastic plates.
Prototype
Jianchen Yu 20

## Slide 24
Niraj Thakker 21
Testing Batteries
Discharge Rate Matters!!
In order to run, the plane requires high instantaneous discharge rate.
Single Layer Lithium Liquid Electrolyte cell can not discharge at a high rate for a long periods of time.
Chart: LiCO Voltage vs. Time at Various Discharge Rates

## Slide 25
Niraj Thakker 22
Testing Batteries
Chart: R.P.M. vs. Static Thurst
| 38.299999999999997 | 85.58 | 152.1 | 237.7 | 342.3 | 465.9 | 608.6 | 770.2 | 950.9
 | 2000 | 3000 | 4000 | 5000 | 6000 | 7000 | 8000 | 9000 | 10000
 | 2000 | 3000 | 4000 | 5000 | 6000 | 7000 | 8000 | 9000 | 10000
Static Thrust
  Static thrust is a function of propeller R.P.M, diameter and pitch.
  (To Sustain Flight)
  (To Take off)
Green Line : 8 x 6 inch propeller
Yellow Line : 9 x 7 inch propeller
Find minimum R.P.M for a given Static Thrust and hence for a given weight of the plane

## Slide 26
Niraj Thakker 23
Testing Batteries
Different battery designs were attached to the motor and the propeller R.P.M was measured.
Tachometer readings were taken every 5 seconds for 6 minutes.
Data for Origami, Large Bent and Stock batteries was obtained.

## Slide 27
Niraj Thakker 24
Testing Batteries
Chart: RPM for Different Battery Designs
Origami | 5307.6667 | 5162 | 5077.3333 | 4961.3333 | 4893.3333 | 4852 | 4827.3333 | 3243.3333 | 3223.6667 | 3227.6667 | 3206.6667 | 3200.6667 | 0
 | Diameter (in) | Pitch (in) | Plane Weight (g) | Minimum Thrust (g) | Minimum R.P.M
Original Battery | 8 | 6 | 485 | 161.67 | 3907.6
 | 9 | 7 |  |  | 3645.1
Origami Cell | 8 | 6 | 606 | 202 | 4388.3
 | 9 | 7 |  |  | 4072.1
Large Bent Cell | 8 | 6 | 753 | 376.5 | 6246.7
 | 9 | 7 |  |  | 5754.8
For Large Bent Cell, the plane will sustain flight for at least 6 minutes
For Origami Cell, the plane will sustain flight for close to 50 seconds

## Slide 28
Large Thin Cells Demo
Jenna Pine 25
For the RC plane application, bending around the wing does not disrupt center of gravity.
Packs connected in series.
Design allows for surface conformability.

## Slide 29
Jenna Pine 26
Large Thin Cells Test Flight

## Slide 30
Origami Prototype Demo
Jenna Pine 27
To give shape conformability smaller cells were connected in parallel to make each pack.
Packs would then be connected in series.
Allows for many different shapes including folding and wrapping.

## Slide 31
Environmental Hazards
Jenna Pine 28
Proper disposal of used materials.
Harmful if electrolyte comes in contact with your skin.
Not good for the ground.

## Slide 32
Safety Hazards
Electrolyte material is extremely flammable and toxic if inhaled.
Can be extremely dangerous if a Lithium Polymer battery is cut open.
Batteries can combust due to improper charging/discharging.
Jenna Pine 29

## Slide 33
Brian Rainbeau 30
Conclusion
Two directions: focused on building cells, while building packs from pre-made cells to validate our design.
Built working thin cells, and integrated others into usable conformable battery packs.

## Slide 34
Future Recommendations
Learn to walk before you run.
Learn to build good ordinary batteries before you attempt to build unique and innovative ones.
Even before the design process, learn the limitations of the technique, facility, and equipment.
Brian Rainbeau 31

## Slide 35
Future Recommendations
Essentially 4 Challenges to overcome
  Build Reliable cells
  Batteries must be light
  Batteries must be powerful
  Accommodate an odd shape
Brian Rainbeau 32

## Slide 36
Questions ?

## Slide 37
Gantt Chart

## Slide 38
Budget Status
Description | Quantity | Unit Price ($) | Total ($)
Ares Gamma 370 RTF plane | 1 | 129.99 | 129.99
Wing Set | 2 | 39.98 | 79.96
Large EPP foam glue | 2 | 9.98 | 19.96
Li-Ion Battery Cathode - Aluminum foil double coated LiFePO4 | 2 | 79.95 | 159.90
Li-Ion Battery Anode - Copper foil double side coated Graphite | 2 | 59.95 | 119.90
FALL TOTAL |  |  | $509.71
Li-Ion Battery Cathode - Aluminum foil double coated LiFePO4 | 1 | 79.95 | 79.95
Li-Ion Battery Anode - Copper foil double side coated Graphite | 1 | 59.95 | 59.95
Polymer Lithium-ion battery (small) 200 mA | 30 | 10.00 | 300.00
Polymer Lithium-ion battery (large) 2800 mA | 6 | 28.00 | 168.00
Battery Charger | 1 | 35.50 | 35.50
Replacement parts and supplies | 1 | 80.96 | 80.96
SPRING TOTAL |  |  | $724.36
GRAND TOTAL |  |  | $1234.07
REMAINING BUDGET |  |  | $765.93

## Slide 39
Why can we not use LiCO cells to fly the plane?
  Handcrafted LiCO cells only provide 8.5mAh capacity per gram of battery. For the battery to supply enough capacity to support its weight and the weight of the plane, the minimum required weight to capacity ratio is 1g to 15 mAh

## Slide 40
Static Thrust Equation