## Slide 1
The nation's annual cost of eye and vision disorders is more costly than three of the top seven major chronic illnesses, including heart disease, Alzheimer's, diabetes and cancer.
Up to 80% of lens wearers experience discomfort causing 30-50% discontinuation of wear cases
90% of the comfort agent market uses eye drops as the delivery system but this approach is inefficient (typically <7% is absorbed by the eye)
More effective comfort agent delivery system lies in controlled release via contact lenses
Engineering Comfortable Contact Lenses: Controlled Release of Comfort Agents
Desmond Pressey, Charles White, Mark E. Byrne
1. Biomimetic & Biohybrid Materials, Biomedical Devices, and Drug Delivery Laboratories,
Department of Chemical Engineering
2. NSF REU Site in Micro-Nano Structured Materials, Therapeutics, and Devices , Auburn University, Auburn, AL 36849, USA
INTRODUCTION
ACKNOWLEDGEMENTS
CONCLUSION
REFERENCES
RESULTS
MOTIVATION
A molecular approach was exercised using polymer contact lenses that serve to hold and release comfort agents to the eye
Enhanced control of ocular comfort agent release can be achieved by engineering contact lenses via molecular imprinting, which involve the formation of a pre-polymerization complex between the template molecule and functional monomers with specific chemical structures designed to have non covalent interactions with the template.
Controlled release of comfort agents via molecularly imprinted contact lenses can solve the need for more efficient topical treatment
The results show that using molecularly imprinted lenses is an efficient method for the release of comfort agents
Trehalose lenses released for a range of 13-16 hours, making it efficient for lenses with made for short durations of wear.
Further innovative testing methods are needed to achieve near authentic conditions related to contact wear in the eye, such as dynamic flow rate, temperature control, oxygen exposure, etc.
Further research will include multi-comfort agent lenses, therapeutic drug releasing lenses, as well as many other applications of molecularly imprinted contact lenses
This research was funded by the National Science Foundation. We thank the NSF REU program, along with the program directors Dr. Mark Byrne and Dr. Steve Duke. We thank the Biomimetic & Biohybrid Materials, Biomedical Devices, & Drug Delivery Laboratories, Auburn University. Thank you to Charles White for needed sample recordings and the rest of Byrne Lab
NSF EEC Award #1063107
C.J. White, A. Tieppo, M.E. Byrne. Controlled drug release from contact lenses: a comprehensive review from 1965-present, J. DRUG DEL. 21 (2011) 369-384.
A. Tieppo, C.J. White, A.C. Paine, M.L. Voyles, M.k. McBride, M.E. Byrne. Sustained in vivo release from imprinted therapeutic contact lenses, Journal of Controlled Release. 157 (2012) 391-397.
Arianna Tieppo, Kayla M. Pate, Mark E. Byrne. In vitro controlled release of an anti-inflammatory from daily disposable therapeutic contact lenses under physiological ocular tear flow, European Journal of Pharmaceutics and Biopharmaceutics 81 (2012) 170–177.
MOLECULAR IMPRINTING
Create polymer lens via molecular imprinting
  Molecular imprinting is the creation of memory within a polymer structure, using functional monomers, templates, and crosslinkers
  Conducting comfort agent releases through polymer lenses with same molecularly imprinted system, but with different mass ratios of functional monomer to comfort agent
Potential in comfort agent lenses
Increased bioavailability
Facilitates patient’s treatment administration
Consistent lubrication levels
Reduced effect from high turnover rate
Figure 1: Graphical assessment of increased efficacy of contact lenses as a controlled comfort agent delivery system
Byrne Lab’s molecular imprinted therapeutic contact lenses are first to demonstrate a successful drug release via contact lenses in animal testing [2]
Figure 2. Molecular imprinting technique.
MATERIALS AND EXPERIMENTAL METHODS
SYNTHESIS OF MOLECULARLY IMPRINTED CONTACT LENSES
Hydrogel contact lenses were synthesized with varying functional monomer to template mass (M/T) ratios (up to 6) using free-radical UV photopolymerization with a given base composition of monomeric species and Trehalose. The mass ratio of crosslinker species to Trehalose was constant at 1.7.
LARGE VOLUME MODEL
PHYSIOLOGICAL FLOW MODEL
DESIGN AND FABRICATION OF MICROFLUIDIC DEVICE
A microfluidic device was engineered and fabricated using polydimethylsiloxane (PDMS).
The device has an inner chamber and two channels for flow. Where the comfort agent lens was placed over a mount and the device was sealed against a glass plate.
IN VITRO DICLOFENAC RELEASE STUDIES
The trehalose-loaded lens was placed within the chamber of the microfluidic device.
A syringe pump was used to pump artificial lacrimal fluid (6.78 g/L NaCl, 2.18 g/L NaHCO3, 1.38 g/L KCl, 0.084 g/L CaCl22 H2O, pH 8), through the device at the physiological flow rate of 3 µL/min.
The samples were collected at regular time intervals.
The trehalose-loaded lenses were placed in a minimum of 250 mL of various release media (deionized water, artificial lacrimal solution, and sterile saline) and kept at 34 C and agitated at 30 rpm in a dissolution apparatus from SOTAX Inc.
The amount of Trehalose in each sample was determined via USP recommended colorimetric UV-Vis Assay.
Chart: Large Volume Release Time (Hours)
| 0.05 | 0.39 | 1.33 | 3.15 | 6.17
M/T - 4 | 1.92 | 3.23 | 5.42 | 9.1 | 15.27
M/T - 3 | 0.9 | 1.82 | 3.67 | 7.39 | 14.88
M/T - 2 | 0.059 | 1.29 | 2.83 | 6.21 | 13.63
Chart: Time (Hours)
| 0.16666666666666666 | 0.33300000000000002 | 0.5 | 0.75 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
M/T - 0 | 72 | 94 | 97 | 93.6 | 98 | 99 | 97 | 99 | 98 | 101 | 100 | 97
M/T - 0.5 | 58 | 64 | 78 | 94 | 100 | 100 | 98 | 99 | 101 | 98 | 100 | 99
M/T - 2 | 44 | 46 | 52 | 65 | 72 | 79 | 84 | 87 | 92 | 91 | 96 | 100
M/T - 3 | 38 | 42 | 49 | 58 | 62 | 69 | 82 | 88 | 92 | 94 | 98 | 100
M/T - 4 | 30 | 38 | 44 | 49 | 59 | 67 | 79 | 88 | 92 | 100 | 99 | 98
M/T - 5 | 22 | 36 | 42 | 46 | 54 | 62 | 76 | 84 | 94 | 100 | 101 | 99
M/T - 6 | 24 | 39 | 47 | 55 | 59 | 64 | 78 | 84 | 96 | 99 | 100 | 98
Chart: Time (Hours)
| 0.16666666666666666 | 0.33300000000000002 | 0.5 | 0.75 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
M/T - 4 - DI Water | 30 | 38 | 44 | 49 | 59 | 67 | 79 | 88 | 92 | 100 | 99 | 98
M/T - 4 - Artificial Lacrimal Solution | 42 | 50 | 48 | 56 | 61 | 72 | 84 | 86 | 94 | 96 | 100 | 100
M/T - 4 - Sterile Saline | 32 | 44 | 46 | 52 | 66 | 69 | 88 | 86 | 92 | 101 | 100 | 99
Chart: Time (Hours)
| 1.5 | 2.5 | 5 | 8 | 14 | 16
M/T - 2 - Microfluidic Device (n = 3) | 43 | 56 | 76 | 92 | 99 | 100
M/T - 3 - Microfluidic Device (n = 3) | 36 | 45 | 73 | 83 | 98 | 100
M/T - 4 - Microfluidic Device (n = 3) | 14.7 | 26 | 54 | 78 | 98 | 100
Figure 3: Picture of Molecularly Imprinted Contact Lens
Figure 4: Picture of Microfluidic Device
Figure 5: Large Volume Model schematic
Figure 6: Physiological Flow Model schematic
Figure 7: Trehalose release studies A & B. Poly(DMS-R11-co-TRIS-co-DMA-co-EGDMA-co-PEG200DMA-co-AA)/Hydrogel Lenses. (A) N=3, 250mL, water exchange at regular time intervals, DI water, and T=34°C. (B) N=3, 3µL/min, samples taken at regular time intervals, and T=22°
Figure 8: Trehalose release study in large volume conditions with various release media. N=3, 350mL, media exchange at regular time intervals, DI water, and T=34°C.
Figure 9: Correlation Plot of release time in physiological flow model vs. large volume model. Created using trend lines from Figure 7 and Figure 8.
Large Volume Model (A)
EFFECT OF RELEASE MEDIA Large Volume Model
Physiological Flow Model (B)
EXAMINING THE EFFECT OF M/T RATIOS
Correlation of Testing Models
Minimal effect of different release media
M/T Ratio
Release Rate