## Slide 1
Shear Strength of Soil
By
Kamal Tawfiq
Fall 2019

## Slide 2
What are the stress vs. strain relationships for materials ????????
Linear Elastic
Nonlinear Elastic
Elastic Plastic
Plastic
Rigid Plastic
What is the strength of any material ????????
Upper limit of the stress – Strain relationship
Why shear strength in soil ?????????
Compressive strength of soil is good
No tensile strength
Shear strength is the most critical
Questions:
Shear Strength
Pick strength
Stress = s
Strain = e
Soft Soil
(Loose sand & normally consolidated Clay)
Stiff Soil (Stiff sand and overconsolidated soil)
Two types of Soil when it comes to stress vs. strain relationships
Peak Strength
Residual Strength
Shear Stresses
Normal Stresses

## Slide 3
Determination of Soil Strength Parameters ( c and f ) in the Lab
1- Direct Shear Test
2- Unconfined Compression Test
3- Triaxial Compression Test
2- Consolidated Undrained Test (CU)
3- Consolidated Drained Test (CD) – Slow Test – Long Term Analysis
1- Unconsolidated Undrained Test (UU) – Quick Test – Short Term Analysis
Fine Soils
sn
t
Mohr-Coulomb Domain
f
sn
t
c
t = c + sn tan f
Yield Surface
Or
Failure Envelope
Mohr-Cuolomb
Yield Criterion
Soil Shear Strength
What is shear strength ????
Soil in weak in shear
To determine the shear strength of soil Mohr-Coulomb Yield Criterion is used
t = c + sn tan f
Soil Cohesion
Angle of Friction
Normal Stress

## Slide 4
I – Direct Shear Test

## Slide 5
D = Horizontal Displacement
N
T
Shearing Force
Normal Force
1- Direct Shear Test
Dial Gage
Dial Gage
Dial Gage
To determine horizontal displacement (Dh)
To determine shearing Load (T)
N
To determine vertical displacement (Dv)

## Slide 6
Shearing Force = T
Normal Force = N
Soil
Shear Resistance
= Angle of
Internal
Friction
Cohesion = c
σn
τ = c + σ tan ϕ

σn1
σn2
σn3
Direct Shear Test
tmax
Δ
σn1 = N/A
 = T/A
tmax1
tmax2
tmax3
By Kamal Tawfiq, Ph.D., P.E.
Repeat this test three times.
Each time increase “N”
- Record sn and tmax for each test
Plot sn and tmax for each test
Fit a straight line through the 3 points
Find c and f

Δ = displacement

## Slide 7
D
t
s1
t1 Failure
D
t
s2
t2 Failure
D
t
s3
t3 Failure
Test # Normal Stress (sn) Shear at Failure (t)
1
2
3
f
t1
t2
t3
s1
s2
s3
sn
t
c
t = c + sn tan f
Direct Shear Test
Angle of Frication
Cohesion
s1
s2
s3
t1
t2
t3
D
t = T/A
sn = N/A
t Failure
t peak
t res
c - f Soil
Example: Sandy - Clay

## Slide 8
D
t
s1
t1 Failure
D
t
s2
t2 Failure
Test # Normal Stress (sn) Shear at Failure (t)
1
2
3
f
t1
t2
t3
s1
s2
s3
sn
t
t = sn tan f
Direct Shear Test
Angle of Frication
s1
s2
s3
t1
t2
t3
t4
s4
D
t
s3
t3 Failure
f Soil
C = 0
Example: Sand

## Slide 9
D
t
s1
t1 Failure
Test # Normal Stress (sn) Shear at Failure (t)
1
2
3
t1
t2
t3
s1
s2
s3
sn
t
t = c
Direct Shear Test
s1
s2
s3
t1
t2
t3
s4
c - Soil
C
f =0
D
t
s2
t2 Failure
D
t
s3
t3 Failure
Example: Clay

## Slide 10
II - Unconfined Compression Test

## Slide 11
Unconfined Compression Test
e
Ds
Ds Failure
Deviator Stress
sn
t
t = cu
s1
qu = s1
Cu = qu/2
qu = Unconfined compressive strength
Cu = Unconfined shear strength
Cu = qu/2
a = 45o + f/2
f = 0
a = 45o
= 0
Failure Surface

## Slide 12
Unconfined Compression Test

## Slide 13
III - TRIAXIAL COMPRESSION TEST

## Slide 14
TRIAXIAL COMPRESSION TEST
Failure Surface
By Kamal Tawfiq, Ph.D., P.E.
a = 45o + f/2

## Slide 15
Cohesion =
c
F
1
F
2
F
n
F
1
F
2
F
1
J
2
F
2
Triaxial Compression Test
Each Circle
=
One Test
Failure Surface
By Kamal Tawfiq, Ph.D., P.E.
F
2
+
F
2
)
F
F
2
+
F
2
)
F
F
2
F
2
F
2
F
2
F
2
2
+
F
2
)
F
f
F
2
+
F
2
)
F
f
=
F
1
=
F
1
3- At Failure
2- Loading
1- Applying
Confining
Stresses
F
1
= Major
Principle Stress
F
2
= Minor Prencipal Stress
)F
= deviator stress
Confining stress
=
Failure
Surface
Deviator stress
=
Axial
stress

## Slide 17
Step 1
Step 2
Triaxial Compression Test
1- Consolidated Undrained Test (CU)
fu
sn
t
cu
t= c + sn tan f
e
Ds
s2
Ds Failure
s2
s1
s2
s1
s2
s1
s1 - s2
s1 - s2
s2
s2
s2
s2
s2
s2
s2
s2
s2
s2
Confining
Pressure
Ds
Ds
Ds
s1 = Ds + s2
Deviator Stress
s2
s2

## Slide 18
Step 1
Step 2
Triaxial Compression Test
2- Consolidated Drained Test (CD)
fd
sn
t
cd
t= c + sn tan f
s2
s1
s2
s1
s2
s1
s1 - s2
s1 - s2
s2
s2
s2
s2
Confining
Pressure
s1 = Ds + s2
s2
Ds
Ds
s2
s2
e
Ds
s2
Ds Failure
Deviator Stress

## Slide 19
Triaxial Compression Test
3- Unconsolidated Undrained Test (UU)
Step 1
Step 2
sn
t
cu
t= c
s2
s1
s2
s1
s2
s1
s1 - s2
s1 - s2
s2
s2
s2
s2
Confining
Pressure
s1 = Ds + s2
s2
Ds
Ds
s2
s2
e
Ds
s2
Ds Failure
Deviator Stress